## Slide 1: 1T- TaS2 through STM and FFT

## Slide 2
What is 1T-TaS2?
The integer indicates the number of X-T-X sandwiches per unit cell along the hexagonal c axis
T is trigonal symmetries
The 1T phase contains X-T-X sandwiches in which the metal atoms are octahedrally coordinated
Polytypes consist of one or more than three-layer sandwiches, inner layer of metal enclosed by layers of chalcogenide atoms
The layers of the sandwiches arranged in hexagonal closed-packed planes
Figure 1: Crystal structure of 1T-TaS2. The hexagonal unit-cell is represented in red. Adapted from ”. “Watching the birth of a charge density wave order: diffraction study on nanometer-and picosecond-scales”. https://www.researchgate.net/publication/315515510_Watching_the_birth_of_a_charge_density_wave_order_diffraction_study_on_nanometer-and_picosecond-scales/figures?lo=1

## Slide 3
Phases in 1T-TaS2
Nearly Commensurate phase (NC Phase):
  the CDW is at an average angle which causes it to be incommensurate with the underlying atomic lattice
  Angle varies with temperature, changing from 11° to 13°
Incommensurate phase (I Phase):
  The CDW is aligned with the lattice, although the CDW wavevector is incommensurate
  Wavelength 3.53 a0 (a0 is the lattice constant of 3.346 Å)
Commensurate phase (C Phase): the CDW is completely commensurate with the underlying tantalum lattice
  Wavelength 3.606 a0
Triclinic phase (T Phase)
  CDW loses its hexagonal symmetry
  The domains are very long and narrow, providing a larger number of CDW maxima (or minima)

## Slide 4
Figure 2: Thomson, R.E, B. Burk, A. Zettl, John Clarke. “Scanning tunneling microscopy of the charge-density-wave structures in 1T-TaS2”

## Slide 5
Data Categorization

## Slide 6
CDW and lattice peaks

## Slide 7
CDW and domain peaks
At room temperature
Chart: Angle between CDW and Domain
| 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 294.3 | 356.13 | 356.12 | 356.1 | 356.18 | 356.11 | 356.49 | 356.51 | 357.35 | 358.19
Warming | 3.2 | 7.5 | 8.3 | 3.7 | 5.1 | 7.1667 | 8.3333 | 6.6667 | 6.5667 | 6.2667 | 6.5 | 4.345 | 18.6333 | 16.1333 | 20.5 | 17.0333 | 18.6333 | 18.4333 | 18 | 22.1 | 15.5667
Cooling | 10.2 | 9.75 | 15.5 | 16.6
(*) Harder to find domain in Cooling down process

## Slide 8
Interesting Data Points
#6120: topography
#6122: topography

## Slide 9
Interesting Data Points
#6120: FFT
#6122: FFT

## Slide 10
Interesting Phase Change
Warming Up
  4751 - 4781: NC Phase (357.5K)
  4782 - 5145: IC Phase (359.30K)
  5146 - 5303: NC Phase (359.14K)
  5304 – 5591: IC Phase (359.30K)
    5311 and 5312: IC Phase
(*) There are images that do not have a good indication of what phase is it (only show CDW).
Cooling Down
  5591 – 6032: IC Phase (359.30K)
  6033 – 6107: IC Phase (356.61K)
  6125 – 6201: NC Phase (356.2K)

## Slide 11
Warming Up
#4789: 359.23K

## Slide 13
Beauty FFT images
NC Phase
#1403: Room Temp

## Slide 14
#2509: 356.13 K

## Slide 15
IC Phase
#1819 362.45

## Slide 16
#4311: 356.61K
IC Phase with a hint of domain

## Slide 17
Reference List
“Watching the birth of a charge density wave order: diffraction study on nanometer-and picosecond-scales”. Retrieved from https://www.researchgate.net/publication/315515510_Watching_the_birth_of_a_charge_density_wave_order_diffraction_study_on_nanometer-and_picosecond-scales/figures?lo=1
Thomson, R.E, B. Burk, A. Zettl, John Clarke. “Scanning tunneling microscopy of the charge-density-wave structures in 1T-TaS2”